Supporting Information

Prediction of Lattice Thermal Conductivity

with Two-stage Interpretable Machine Learning

Jinlong Hu,1, † Yuting Zuo,1, † Yuzhou Hao,1, † Guoyu Shu,1 Yang Wang,1 Minxuan Feng,1 Xuejie Li,1 Xiaoying Wang,1 Jun Sun,1 Xiangdong Ding,1  Zhibin Gao,1, ∗, Guimei Zhu,2 and Baowen Li2, §

1 State Key Laboratory for Mechanical Behavior of Materials,

Xi’an Jiaotong University, Xi’an 710049, China

2 Department of Materials Science and Engineering,

Department of Physics. Southern University of Science and Technology, Shenzhen,

518055, PR China. International Quantum Academy, Shenzhen 518048,

PR China. Paul M. Rady Department of Mechanical Engineering and Department of Physics, University of Colorado, Boulder, Colora

FIG. S1. Comparisons of the predicted and calculated values of shear modulus on testing datasets with a different number of convolutional layers, and the other hyperparameters such as Epoch, Batchsize and Learning rate are set as the same, i.e., Epoch=30, Batchsize=256, Learning rate=0.010. (a) Comparison of the predicted and calculated values of shear modulus on testing dataset with n=2 convolutional layers, (b) Comparison of the predicted and calculated values of shear modulus on testing dataset with n=3 convolutional layers, (c) Comparison of the predicted and calculated values of shear modulus on testing dataset with n=4 convolutional layers, (d) Comparison of the predicted and calculated values of shear modulus on testing dataset with n=5 convolutional layers. It is noted that the model achieves the best performance when the number of convolutional layers is set to 3. Thus, in this study, the number of convolutional layers n is set to 3 in the following simulations.

FIG. S2. Comparisons of the predicted and calculated values of shear modulus on testing datasets with different learning rates (lr), (a) lr = 0.005, (b) lr = 0.01, (c) lr = 0.015, (a) lr = 0.02, and the other hyperparameters such as Epoch, Batchsize and number of convolutional layers are set as the same, i.e., Epoch=30, Batchsize=256, n=3. It is noted that the model achieves comparable superior performance as the learning rate is set to 0.005, 0.01 and 0.015. However, the model performs poorly when the learning rate increases to 0.02. The fact is that when the learning rate is too large, the model becomes divergent, resulting in poor performance.

FIG. S3. Comparisons of the predicted and calculated values of shear modulus on testing datasets with different learning rates (lr), (a) lr = 0.005, (b) lr = 0.01, (c) lr = 0.015, (a) lr = 0.02, and the other hyperparameters such as Epoch, Batchsize and the number of convolutional layers are set as the same, i.e. Epoch=30, Batchsize=512, n=3. It is noted that the model achieves superior performance as the learning rate is set to 0.01. Furthermore, the performance of the model with batchsize=256 is worse than that of the model with batchsize=128 with the same other hyperparameters. The fact is that large batchsize leads to reduced model generalization ability.

Combining the above study, the hyperparameters of the test dataset in the study were chosen as follows: the number of convolutional layers n was set to 3, the batchsize was set to 256, and the learning rate was set to 0.01. In summary, during the process of model training, neither the learning rate nor the batchsize should be too large or too small, and they need to be adjusted accordingly based on the actual task to obtain the optimal performance.

Table S1. Lattice thermal conductivity prediction of compounds in the OQMD database sorted in ascending order by the value of kL (first 100). Physical parameters shear modulus (G), Grüneisen parameter (γ), the average speed of sound (vm), Bulk modulus (B) are predicted with our proposed method.

| Compound | kL W/mK * | V (10-10 m)3 | N | G 109 kg/ms2 | γ | vm m/s | T K | B 109 kg/ms2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BaBr2 | 0.0001586888 * | 129.205 | 3 | 0.00183 | 2.16085 | 1338.97144 | 300 | 7.005493164 |
| YCl3 | 0.0002884277 * | 249.52 | 8 | 0.00447 | 2.07637 | 1959.78906 | 300 | 11.76267242 |
| RbMnBr3 | 0.0003373089 * | 154.754 | 10 | 0.01696 | 2.45471 | 1293.62671 | 300 | 17.98638153 |
| K2PbCl6 | 0.0003598286 * | 263.739 | 9 | 0.00872 | 2.37823 | 1874.59314 | 300 | 6.207267761 |
| Cs3RbSe2 | 0.0008905375 * | 294.811 | 6 | 0.01515 | 2.1162 | 1319.2522 | 300 | 19.86326599 |
| Cs3RbSe2 | 0.0008907617 * | 294.811 | 6 | 0.01516 | 2.1162 | 1319.2522 | 300 | 19.86326599 |
| Rb2SnCl6 | 0.0009301600 * | 266.013 | 9 | 0.02606 | 2.42199 | 1688.62878 | 300 | 9.532432556 |
| ZrBr2Cl2 | 0.0009658170 * | 324.668 | 10 | 0.02291 | 2.11894 | 1531.06787 | 300 | 7.971298218 |
| K3NdCl6 | 0.0014972381 * | 360.304 | 10 | 0.03038 | 2.17497 | 1828.8396 | 300 | 11.88388062 |
| RbCl | 0.0016919177 * | 62.5338 | 2 | 0.01878 | 2.40993 | 1516.19849 | 300 | 8.676612854 |
| Cs2PbCl6 | 0.0019420122 * | 298.419 | 9 | 0.07464 | 2.4698 | 1242.60315 | 300 | 6.049194336 |
| CsSnBr3 | 0.0022855173 * | 201.023 | 5 | 0.04777 | 2.187 | 1091.42944 | 300 | 12.98477936 |
| KPbBr3 | 0.0028077764 * | 211.806 | 5 | 0.0484 | 2.16454 | 1271.55957 | 300 | 10.84622955 |
| CsK2Br3 | 0.0031479698 * | 248.208 | 6 | 0.07422 | 2.40758 | 1349.3302 | 300 | 11.39260864 |
| Cs2SnBr6 | 0.0031725257 * | 336.233 | 9 | 0.15529 | 2.45362 | 922.59521 | 300 | 11.6121521 |
| Cs3EuCl6 | 0.0032408278 * | 423.768 | 10 | 0.09654 | 2.21639 | 1230.07629 | 300 | 17.03804779 |
| K2IBr | 0.0036799503 * | 167.514 | 4 | 0.05377 | 2.38482 | 1617.45789 | 300 | 13.32219696 |
| Rb2SnCl6 | 0.0044367618 * | 264.12 | 9 | 0.12346 | 2.42079 | 1702.06494 | 300 | 9.859489441 |
| CsMgBr3 | 0.0044671531 * | 158.028 | 5 | 0.08855 | 2.13209 | 1180.24561 | 300 | 18.83285522 |
| Cs2TeBr6 | 0.0046731073 * | 336.514 | 9 | 0.19964 | 2.35937 | 961.71313 | 300 | 6.167961121 |
| Rb2SBr6 | 0.0046787003 * | 304.751 | 9 | 0.1488 | 2.40167 | 1392.98438 | 300 | 5.925880432 |
| K4Br2O | 0.0050774265 * | 221.422 | 7 | 0.07637 | 2.18993 | 2062.03369 | 300 | 16.96526337 |
| NdBr4 | 0.0051447772 * | 354.569 | 10 | 0.15895 | 2.15924 | 1188.69446 | 300 | 10.53346252 |
| Cs2NpBr6 | 0.0051643342 * | 363.355 | 9 | 0.17508 | 2.16232 | 970.04553 | 300 | 7.690986633 |
| Rb2MnBr6 | 0.0052853878 * | 297.451 | 9 | 0.20991 | 2.50788 | 1250.52734 | 300 | 8.895599365 |
| Ba2I3Cl | 0.0053987187 * | 271.888 | 6 | 0.09165 | 2.22868 | 1520.06262 | 300 | 14.29807281 |
| Ba2I3Cl | 0.0053991677 * | 271.888 | 6 | 0.09166 | 2.22868 | 1520.0625 | 300 | 14.29807281 |
| Cs2SnCl4 | 0.0054184625 * | 269.056 | 7 | 0.14839 | 2.42415 | 1341.32532 | 300 | 8.392936707 |
| RbCdCl3 | 0.0055990739 * | 142.54 | 5 | 0.1059 | 2.3077 | 1526.05774 | 300 | 10.39572906 |
| Cs2CaCl4 | 0.0060210291 * | 252.178 | 7 | 0.11581 | 2.20633 | 1569.5249 | 300 | 11.6930542 |
| K2PbCl6 | 0.0060584276 * | 260.14 | 9 | 0.14647 | 2.38517 | 1900.08435 | 300 | 6.409263611 |
| Rb2MnBr6 | 0.0061366149 * | 296.706 | 9 | 0.24354 | 2.50806 | 1252.71582 | 300 | 8.905441284 |
| YCl3 | 0.0067594417 * | 244.928 | 8 | 0.10511 | 2.08027 | 1975.1311 | 300 | 11.70582581 |
| RbCl3 | 0.0067616597 * | 324.364 | 8 | 0.16318 | 2.4306 | 1645.04761 | 300 | 7.708175659 |
| Cs3SmCl6 | 0.0067771931 * | 417.561 | 10 | 0.2034 | 2.24595 | 1263.70203 | 300 | 17.16936493 |
| Rb2MnBr6 | 0.0072421255 * | 294.796 | 9 | 0.28782 | 2.5099 | 1255.92956 | 300 | 9.32875061 |
| KSnBr3 | 0.0073999592 * | 378.716 | 10 | 0.19377 | 2.22334 | 1462.90027 | 300 | 10.9136734 |
| RbCl | 0.0075592560 * | 62.6036 | 2 | 0.08391 | 2.40843 | 1513.23462 | 300 | 8.760742188 |
| Cs2SeCl6 | 0.0079075867 * | 285.988 | 9 | 0.21329 | 2.26141 | 1458.01453 | 300 | 5.796485901 |
| CsCdBr3 | 0.0080928754 * | 351.678 | 10 | 0.31194 | 2.2448 | 1040.7301 | 300 | 10.56188202 |
| Cs2UCl6 | 0.0081281073 * | 301.803 | 9 | 0.24265 | 2.2555 | 1286.31226 | 300 | 8.730613708 |
| RbCdCl3 | 0.0082902256 * | 142.267 | 5 | 0.15662 | 2.30796 | 1529.16785 | 300 | 10.50395203 |
| ZrI2Cl2 | 0.0085458929 * | 380.209 | 10 | 0.20498 | 2.10277 | 1413.75452 | 300 | 10.8176651 |
| RbCl | 0.0086360808 * | 62.5708 | 2 | 0.0959 | 2.40874 | 1513.4021 | 300 | 8.773742676 |
| Cs2PbCl6 | 0.0087245661 * | 300.48 | 9 | 0.33009 | 2.46412 | 1252.25305 | 300 | 6.830337524 |
| Cs2CaCl4 | 0.0087268797 * | 251.639 | 7 | 0.16812 | 2.20742 | 1569.8783 | 300 | 11.79515839 |
| RbCdCl3 | 0.0089138782 * | 143.264 | 5 | 0.16777 | 2.30737 | 1530.45398 | 300 | 9.875671387 |
| RbBr | 0.0089448125 * | 154.701 | 4 | 0.17494 | 2.37745 | 1231.80737 | 300 | 11.296875 |
| Rb2SiBr6 | 0.0090654817 * | 296.412 | 9 | 0.25352 | 2.33704 | 1498.78333 | 300 | 12.75189972 |
| Cs2PdCl4 | 0.0093623634 * | 261.038 | 7 | 0.25203 | 2.40577 | 1353.33106 | 300 | 11.87854004 |
| Rb4IBr3 | 0.0095333337 * | 356.008 | 8 | 0.30161 | 2.46044 | 1253.39343 | 300 | 11.01956177 |
| CsCuBr3 | 0.0098458702 * | 320.564 | 10 | 0.44748 | 2.44895 | 1116.51135 | 300 | 17.5074234 |
| Li2ZrBr6 | 0.0099159775 * | 285.138 | 9 | 0.29332 | 2.26169 | 1331.18494 | 300 | 7.677482605 |
| CsNaCl2 | 0.0103900700 * | 264.673 | 8 | 0.22845 | 2.28731 | 1674.32471 | 300 | 13.34420013 |
| Cs2ThCl6 | 0.0104648183 * | 309.37 | 9 | 0.30964 | 2.25119 | 1281.6073 | 300 | 6.567108154 |
| Na2SnCl6 | 0.0107190305 * | 238.856 | 9 | 0.22735 | 2.357 | 2166.41553 | 300 | 11.21305847 |
| CsNaCl2 | 0.0109239269 * | 261.875 | 8 | 0.24203 | 2.29135 | 1674.19824 | 300 | 13.20007324 |
| CsGeCl3 | 0.0110097065 * | 299.864 | 10 | 0.29962 | 2.28373 | 1616.21423 | 300 | 12.86406708 |
| K3YCl6 | 0.0113588370 * | 338.814 | 10 | 0.20858 | 2.15101 | 2013.87793 | 300 | 10.80363464 |
| Cs2SeBr6 | 0.0114675237 * | 325.584 | 9 | 0.47755 | 2.33568 | 974.15759 | 300 | 6.017234802 |
| Rb2GeBr6 | 0.0114888601 * | 309.008 | 9 | 0.37262 | 2.36524 | 1310.96387 | 300 | 8.581680298 |
| K3YBr6 | 0.0123554810 * | 409.383 | 10 | 0.28065 | 2.14978 | 1526.63538 | 300 | 17.54858398 |
| K3TlCl6 | 0.0123714146 * | 332.899 | 10 | 0.2987 | 2.29723 | 1783.23755 | 300 | 9.8984375 |
| K3ScBr6 | 0.0124138160 * | 371.251 | 10 | 0.29886 | 2.25607 | 1654.99695 | 300 | 17.100914 |
| UCl4 | 0.0124401174 * | 309.643 | 10 | 0.30848 | 2.17179 | 1569.03967 | 300 | 6.50289917 |
| ZrAg2Cl6 | 0.0125372155 * | 229.684 | 9 | 0.31494 | 2.26884 | 1696.83386 | 300 | 24.80099487 |
| RbNaCl2 | 0.0128195379 * | 254.426 | 8 | 0.24869 | 2.24673 | 1846.33496 | 300 | 14.68782043 |
| Cs2HgCl4 | 0.0130109405 * | 279.466 | 7 | 0.4268 | 2.4387 | 1121.94238 | 300 | 10.1056366 |
| Rb2GeBr6 | 0.0130177440 * | 306.504 | 9 | 0.42282 | 2.36752 | 1315.61487 | 300 | 9.020889282 |
| CsMnBr3 | 0.0133063627 * | 160.044 | 5 | 0.37457 | 2.42504 | 1109.32849 | 300 | 17.81276703 |
| Rb3CrCl6 | 0.0133196745 * | 313.204 | 10 | 0.35536 | 2.34937 | 1735.10828 | 300 | 11.58808136 |
| Rb2SiBr6 | 0.0133655176 * | 293.717 | 9 | 0.37407 | 2.33901 | 1505.13354 | 300 | 13.17882538 |
| Rb3AsCl6 | 0.0133886688 * | 341.827 | 10 | 0.35247 | 2.27286 | 1582.08301 | 300 | 10.80644989 |
| Cs2PuCl6 | 0.0136212611 * | 297.459 | 9 | 0.38655 | 2.21528 | 1306.1283 | 300 | 7.629714966 |
| CsHgBr3 | 0.0142468787 * | 362.652 | 10 | 0.84696 | 2.44829 | 818.64185 | 300 | 11.06295776 |
| RbSnBr3 | 0.0147157002 * | 388.64 | 10 | 0.52412 | 2.33446 | 1191.599 | 300 | 13.4677124 |
| NaIn3Br6 | 0.0148254207 * | 340.153 | 10 | 0.46265 | 2.25107 | 1308.02551 | 300 | 18.28351593 |
| MgCl2 | 0.0152675786 * | 76.6194 | 3 | 0.10813 | 2.04528 | 2313.23096 | 300 | 16.27352142 |
| Rb2PdI4 | 0.0153880613 * | 333.772 | 7 | 0.44893 | 2.44574 | 1197.43042 | 300 | 11.39046478 |
| CsBaI3 | 0.0158735254 * | 310.975 | 5 | 0.37279 | 2.41979 | 1059.97742 | 300 | 16.13456726 |
| Cs2ZrI6 | 0.0159272664 * | 426.131 | 9 | 0.5119 | 2.26057 | 1070.43005 | 300 | 8.511993408 |
| Cs2CoBr6 | 0.0162109362 * | 304.641 | 9 | 0.68344 | 2.44165 | 1093.79138 | 300 | 9.425086975 |
| RbHgCl3 | 0.0163173980 * | 309.597 | 10 | 0.67916 | 2.50189 | 1300.42822 | 300 | 10.53633118 |
| ScBr3 | 0.0163484775 * | 247.402 | 8 | 0.32684 | 2.11791 | 1589.80408 | 300 | 12.40502167 |
| CsCaCl3 | 0.0167852788 * | 160.137 | 5 | 0.25689 | 2.17219 | 1584.21985 | 300 | 11.66838837 |
| Cs2SeCl6 | 0.0170693413 * | 285.81 | 9 | 0.45952 | 2.26174 | 1461.66016 | 300 | 6.156341553 |
| CsMnBr3 | 0.0170769168 * | 319.785 | 10 | 0.76609 | 2.43197 | 1112.98633 | 300 | 18.06908417 |
| Ba2NbBr6 | 0.0172412221 * | 271.366 | 9 | 0.45763 | 2.25377 | 1496.33398 | 300 | 6.256263733 |
| CsCaCl3 | 0.0173722495 * | 160.279 | 5 | 0.26588 | 2.17233 | 1583.88928 | 300 | 11.6930542 |
| RbBrCl2 | 0.0173832842 * | 326.239 | 8 | 0.46946 | 2.43461 | 1473.10754 | 300 | 7.763618469 |
| Rb2PdCl6 | 0.0174011665 * | 251.166 | 9 | 0.5104 | 2.47712 | 1737.18689 | 300 | 11.31089783 |
| RbAuBr3 | 0.0175136502 * | 334.103 | 10 | 0.78048 | 2.43456 | 1107.0376 | 300 | 15.9084549 |
| K3InCl6 | 0.0175519953 * | 322.612 | 10 | 0.39411 | 2.2858 | 1915.62695 | 300 | 10.44287872 |
| Rb2GeBr6 | 0.0176798719 * | 309.176 | 9 | 0.57713 | 2.3572 | 1291.86291 | 300 | 8.1509552 |
| RbCrBr3 | 0.0178466281 * | 363.064 | 10 | 0.51425 | 2.27505 | 1419.76892 | 300 | 11.84221649 |
| Rb2PdBr6 | 0.0180306453 * | 292.179 | 9 | 0.72975 | 2.47881 | 1199.08765 | 300 | 9.20740509 |
| Cs2SeCl6 | 0.0181018542 * | 280.827 | 9 | 0.48774 | 2.26632 | 1475.71021 | 300 | 6.88168335 |
| BaBr2 | 0.0181093361 * | 388.066 | 9 | 0.43968 | 2.1782 | 1346.3064 | 300 | 5.770713806 |
| Sr2SnI6 | 0.0181725735 * | 374.623 | 9 | 0.39386 | 2.17052 | 1514.31421 | 300 | 14.78739929 |
| Ba2GeI6 | 0.0182095719 * | 367.486 | 9 | 0.41069 | 2.15748 | 1445.59216 | 300 | 14.13695526 |

Table S2. Lattice thermal conductivity prediction of compounds in the OQMD database sorted in ascending order by the value of kL (first 100). Physical parameters shear modulus (G), Grüneisen parameter (γ), the average speed of sound (vm), Bulk modulus (B) are predicted with our proposed method.

| Compound | kL W/mK * | V (10-10 m)3 | N | G 109 kg/ms2 | γ | vm m/s | T K | B 109 kg/ms2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LuAlO3 | 26.8934446352 * | 48.4125 | 5 | 132.56519 | 1.95194 | 5879.94238 | 300 | 240.4460297 |
| CaO | 26.9173307109 * | 24.5953 | 2 | 71.92405 | 1.97979 | 5591.16357 | 300 | 118.0415039 |
| CaO | 26.9450926242 * | 24.5481 | 2 | 71.96006 | 1.98024 | 5600.24805 | 300 | 118.3086548 |
| CaSiO3 | 27.0461066716 * | 45.6324 | 5 | 117.18576 | 2.00905 | 7223.55713 | 300 | 218.5862122 |
| YbSiO3 | 27.0696848753 * | 44.2432 | 5 | 152.6599 | 1.9689 | 5386.59668 | 300 | 263.6143799 |
| CaSiO3 | 27.0840361491 * | 45.7342 | 5 | 119.30441 | 2.0183 | 7165.88916 | 300 | 222.7526093 |
| CaSiO3 | 27.1993607889 * | 45.7026 | 5 | 117.82535 | 2.00957 | 7225.09619 | 300 | 218.6865387 |
| SiGeO3 | 27.3858171372 * | 51.662 | 5 | 148.49838 | 2.12451 | 6215.88574 | 300 | 238.6772766 |
| BeO | 27.4343005216 * | 56.3528 | 8 | 117.08961 | 1.76212 | 8543.29981 | 300 | 190.2034607 |
| YbBe2N2 | 27.4394571553 * | 44.3081 | 5 | 128.83029 | 1.80872 | 5509.81934 | 300 | 186.5392151 |
| HoAlO3 | 27.6382446896 * | 49.8758 | 5 | 148.71944 | 1.91759 | 5153.1001 | 300 | 249.463974 |
| ScN | 27.7820934513 * | 53.4512 | 4 | 100.24199 | 1.84432 | 5583.27344 | 300 | 188.8366089 |
| HoAlO3 | 28.0148028979 * | 49.6559 | 5 | 149.73506 | 1.91825 | 5198.96289 | 300 | 251.5736694 |
| MgO | 28.1131547914 * | 18.0947 | 2 | 69.97734 | 1.90316 | 6158.15918 | 300 | 155.6996918 |
| MgO | 28.1857413109 * | 18.0784 | 2 | 70.09547 | 1.90304 | 6164.7627 | 300 | 155.8412933 |
| MgO | 28.2366023139 * | 18.067 | 2 | 70.17807 | 1.90295 | 6169.39111 | 300 | 155.9403992 |
| CuBO2 | 28.2945980625 * | 60.0414 | 8 | 176.1958 | 1.99181 | 7213.29053 | 300 | 264.9272766 |
| AlPO4 | 28.3740633187 * | 47.5441 | 6 | 135.66052 | 1.97043 | 7455.10254 | 300 | 236.2902985 |
| HoAlO3 | 28.3843518614 * | 49.4762 | 5 | 150.4975 | 1.91484 | 5229.34375 | 300 | 249.0298004 |
| ErAlO3 | 28.5877584479 * | 49.3364 | 5 | 151.15059 | 1.91701 | 5260.39844 | 300 | 253.1156616 |
| CeBO3 | 28.6337506253 * | 46.4137 | 5 | 148.93866 | 2.04674 | 6212.97168 | 300 | 250.7772064 |
| LaBO3 | 28.6474974142 * | 46.3348 | 5 | 148.80232 | 2.04601 | 6220.6377 | 300 | 250.5484161 |
| SiO2 | 28.6476465501 * | 51.4792 | 6 | 136.44835 | 1.99762 | 7488.67871 | 300 | 262.401062 |
| ErAlO3 | 28.7798325904 * | 49.2265 | 5 | 151.58441 | 1.91534 | 5275.68848 | 300 | 252.7424927 |
| ErAlO3 | 28.8358592308 * | 49.2143 | 5 | 151.68513 | 1.91554 | 5283.97803 | 300 | 252.5653992 |
| BeSiN2 | 28.8533607428 * | 66.9166 | 8 | 138.32674 | 1.86697 | 7976.37744 | 300 | 202.7080078 |
| LaBO3 | 28.8811358452 * | 46.2927 | 5 | 147.55635 | 2.03231 | 6240.19141 | 300 | 245.7484894 |
| BeSiO3 | 28.8866640560 * | 40.9233 | 5 | 112.59676 | 1.96123 | 7937.61133 | 300 | 233.2103577 |
| CeBO3 | 28.9336893799 * | 46.3705 | 5 | 147.75258 | 2.03209 | 6238.39062 | 300 | 245.355896 |
| BeSiN2 | 29.0515843980 * | 66.593 | 8 | 139.02176 | 1.8656 | 7992.97656 | 300 | 203.4050598 |
| ScAlO3 | 29.1106693921 * | 47.2368 | 5 | 133.13692 | 1.94563 | 6349.33789 | 300 | 263.6515808 |
| ScAlO3 | 29.1547189145 * | 47.166 | 5 | 132.36967 | 1.94543 | 6397.7373 | 300 | 262.2631836 |
| TbAlO3 | 29.3730806660 * | 50.3948 | 5 | 150.56485 | 1.9207 | 5407.59912 | 300 | 255.5942841 |
| DyAlO3 | 29.3954668326 * | 50.1346 | 5 | 147.49602 | 1.93213 | 5597.48145 | 300 | 241.6125336 |
| YAlO3 | 29.4966688910 * | 49.8927 | 5 | 148.18208 | 1.93951 | 5641.26025 | 300 | 249.9268494 |
| DyAlO3 | 29.5356226009 * | 50.1108 | 5 | 147.52449 | 1.93127 | 5619.14209 | 300 | 239.9522705 |
| YAlO3 | 29.6307373486 * | 50.4549 | 5 | 149.17038 | 1.93568 | 5586.88867 | 300 | 244.4929047 |
| TbAlO3 | 29.7635314983 * | 50.3272 | 5 | 151.42146 | 1.91657 | 5428.43164 | 300 | 254.2587738 |
| YAlO3 | 29.7761149212 * | 50.3824 | 5 | 149.64734 | 1.93545 | 5597.8501 | 300 | 245.0220184 |
| DyAlO3 | 29.8957724063 * | 49.9312 | 5 | 148.39078 | 1.93034 | 5655.95508 | 300 | 240.6007996 |
| TbAlO3 | 29.9143551237 * | 50.2163 | 5 | 151.87715 | 1.91771 | 5449.83105 | 300 | 255.6404724 |
| YAlO3 | 30.1368462742 * | 50.2053 | 5 | 150.7305 | 1.93469 | 5627.27441 | 300 | 245.9281158 |
| ScN | 30.1440882090 * | 28.8876 | 2 | 78.00867 | 1.91721 | 5139.72119 | 300 | 131.2412415 |
| MgO | 30.5258385646 * | 18.5334 | 2 | 70.08984 | 1.91494 | 6701.31592 | 300 | 136.9517212 |
| BN | 30.6190149628 * | 16.3738 | 2 | 50.15576 | 1.67676 | 7714.59228 | 300 | 113.2483521 |
| MgO | 30.6281515067 * | 18.5095 | 2 | 70.19055 | 1.91486 | 6716.45996 | 300 | 137.1503906 |
| MgO | 30.6713456361 * | 18.4995 | 2 | 70.23302 | 1.91482 | 6722.8335 | 300 | 137.2344055 |
| MgO | 30.6980557510 * | 18.5438 | 2 | 70.26076 | 1.91491 | 6721.27197 | 300 | 137.2455902 |
| MgO | 30.7314629024 * | 18.5031 | 2 | 70.29282 | 1.91481 | 6729.74414 | 300 | 137.3394775 |
| BeO | 30.7878613252 * | 54.584 | 8 | 129.60043 | 1.77711 | 8886.96875 | 300 | 203.341095 |
| BeO | 30.7878613252 * | 54.584 | 8 | 129.60043 | 1.77711 | 8886.96875 | 300 | 203.341095 |
| MgO | 30.9758811328 * | 18.4512 | 2 | 70.53319 | 1.91459 | 6764.99805 | 300 | 137.8174591 |
| EuSiO3 | 31.0353636988 * | 46.327 | 5 | 158.97423 | 1.9856 | 5938.5498 | 300 | 259.6976318 |
| EuSiO3 | 31.1277017522 * | 46.3851 | 5 | 158.83179 | 1.98375 | 5948.00049 | 300 | 256.6190796 |
| TmAlO3 | 33.0256845123 * | 48.9847 | 5 | 158.83562 | 1.90719 | 5740.18457 | 300 | 275.0955505 |
| SiO2 | 33.0301632098 * | 23.355 | 3 | 111.24379 | 2.16478 | 8145.19043 | 300 | 231.9875031 |
| TmAlO3 | 33.4007068088 * | 48.851 | 5 | 159.75462 | 1.90609 | 5770.87744 | 300 | 275.2298279 |
| AlN | 33.5529299747 * | 41.8633 | 4 | 118.68445 | 1.89077 | 6472.29199 | 300 | 197.6177979 |
| AlN | 33.5529787130 * | 41.8633 | 4 | 118.68452 | 1.89077 | 6472.29492 | 300 | 197.6179199 |
| AlN | 33.5581681013 * | 41.8622 | 4 | 118.71146 | 1.89083 | 6472.24512 | 300 | 197.6329346 |
| BN | 33.5773670271 * | 71.0418 | 8 | 123.21434 | 1.72419 | 8855.88086 | 300 | 182.7440796 |
| AlN | 33.6504053533 * | 41.757 | 4 | 119.08963 | 1.89073 | 6474.20215 | 300 | 197.9427795 |
| TmAlO3 | 33.6580201530 * | 48.8722 | 5 | 160.49554 | 1.9051 | 5781.9248 | 300 | 273.7223511 |
| MgO | 33.8510127797 * | 19.2817 | 2 | 74.30579 | 1.9095 | 6880.2168 | 300 | 151.1708679 |
| MgO | 33.8517684635 * | 19.2816 | 2 | 74.30656 | 1.90949 | 6880.29688 | 300 | 151.1731262 |
| SiGeO3 | 34.2062124114 * | 45.9671 | 5 | 159.8629 | 2.1148 | 7425.82764 | 300 | 277.3581238 |
| MgO | 34.2626558485 * | 19.1109 | 2 | 74.88892 | 1.90801 | 6919.92285 | 300 | 152.6387787 |
| AlN | 37.8839763785 * | 67.8575 | 8 | 180.24858 | 1.88552 | 8149.52734 | 300 | 248.1051483 |
| SiO2 | 40.3373450403 * | 46.8378 | 6 | 165.76888 | 1.9872 | 8864.20898 | 300 | 299.1691284 |
| SiO2 | 40.4688118512 * | 47.0431 | 6 | 166.65848 | 1.98951 | 8853.22266 | 300 | 299.0551758 |
| Si2O3 | 40.8042832107 * | 44.8829 | 5 | 162.56677 | 2.03507 | 8107.56445 | 300 | 282.3444214 |
| MgBe2N2 | 43.9585964661 * | 37.7965 | 5 | 127.23366 | 1.74954 | 8882.42773 | 300 | 183.2398682 |
| AlHO2 | 44.9564984912 * | 27.5558 | 4 | 131.0164 | 1.84635 | 8638.45801 | 300 | 222.2664795 |
| BeO | 48.9582659122 * | 27.3284 | 4 | 129.75044 | 1.77716 | 8888.67969 | 300 | 203.4122009 |
| BeO | 49.0360666195 * | 27.2986 | 4 | 129.8784 | 1.77728 | 8898.38672 | 300 | 203.586792 |
| AlN | 51.1636108163 * | 20.9876 | 2 | 116.76358 | 1.91102 | 6443.11328 | 300 | 194.5191345 |
| AlN | 51.4298368514 * | 20.9028 | 2 | 117.5304 | 1.91136 | 6445.2998 | 300 | 195.3581085 |
| AlN | 52.0361167116 * | 38.9426 | 4 | 156.54196 | 1.88306 | 7736.01123 | 300 | 219.1294556 |
| AlN | 52.7714725397 * | 38.9821 | 4 | 158.12177 | 1.88293 | 7763.27588 | 300 | 220.484726 |
| BN | 55.7866203144 * | 53.2123 | 8 | 193.99229 | 1.74654 | 10522.86621 | 300 | 284.7519836 |
| AlN | 57.9866077771 * | 33.168 | 4 | 176.42206 | 1.88629 | 8095.69189 | 300 | 239.3661041 |
| BN | 62.1254314607 * | 49.0838 | 8 | 218.33948 | 1.7474 | 10705.05859 | 300 | 297.9784546 |
| SiO2 | 68.4745241769 * | 26.8731 | 3 | 190.34001 | 2.02542 | 8192.81152 | 300 | 288.2576294 |
| SiO2 | 70.8237201599 * | 28.3995 | 3 | 202.06335 | 2.07291 | 8217.67676 | 300 | 280.5477905 |
| BeO | 76.1339645986 * | 13.7009 | 2 | 128.05698 | 1.77589 | 8803.80469 | 300 | 201.6268311 |
| BeO | 76.3461129878 * | 13.6872 | 2 | 128.28398 | 1.77609 | 8817.41211 | 300 | 201.8978882 |
| AlN | 91.6195534846 * | 16.6135 | 2 | 175.8757 | 1.88689 | 8083.15772 | 300 | 238.7668152 |
| AlN | 91.9774855102 * | 16.5897 | 2 | 176.32741 | 1.88638 | 8093.65576 | 300 | 239.2722626 |
| AlN | 92.1198981718 * | 16.5772 | 2 | 176.52792 | 1.88621 | 8097.60498 | 300 | 239.4452057 |
| BeO | 96.1448371471 * | 12.8567 | 2 | 144.74553 | 1.76205 | 9908.57715 | 300 | 247.4322815 |
| BeO | 96.6181539937 * | 12.8277 | 2 | 145.13618 | 1.76147 | 9932.25781 | 300 | 247.6124268 |
| BN | 119.4468846432 * | 23.4882 | 4 | 263.97583 | 1.76766 | 11105.23535 | 300 | 316.4334106 |
| BeO | 130.5891297036 * | 12.621 | 2 | 183.28806 | 1.79119 | 11010.29297 | 300 | 224.3136749 |
| BeO | 154.8848247205 * | 11.8316 | 2 | 209.28206 | 1.78489 | 11612.16797 | 300 | 238.8886108 |
| BeO | 155.0781826501 * | 11.803 | 2 | 209.3049 | 1.78442 | 11629.38672 | 300 | 238.9816284 |
| BeO | 155.1842534524 * | 11.7869 | 2 | 209.27531 | 1.78426 | 11642.36914 | 300 | 238.9738617 |
| BN | 187.5920446893 * | 11.6911 | 2 | 261.66437 | 1.76607 | 11083.1875 | 300 | 314.5681152 |
| BN | 189.2397749820 * | 11.7311 | 2 | 263.05057 | 1.7649 | 11095.92383 | 300 | 316.699646 |
| BN | 189.2876467635 * | 11.7323 | 2 | 263.09021 | 1.76486 | 11096.2832 | 300 | 316.762207 |
| BN | 189.6874805298 * | 11.7425 | 2 | 263.41959 | 1.76456 | 11099.24414 | 300 | 317.2870483 |